**Basic variant for wet installation**

for buildings with a basement

For joint entry and sealing of all supply lines (power/water/telecommunications/gas), installation by means of casting in core drill holes with ∅ 200 mm in difficult wall materials (e.g. masonry, brick, aerated concrete). The MSH PolySafe - MV (grouting) is supplemented with closed sealing elements which are available to purchase separately. The following components are necessary for installation: Compound injection unit MSH PolySafe Void-filling mortar MSH PolySafe - VM

Dimensions: Sealing width: 30 mm; Compatible with core drill/wall sleeve: ID: 199 - 203 mm; Maximum wall thickness: 500 mm (special lengths on request)

Material: Inner seal: Fibre-glass reinforced polyamide/EPDM; Sleeve pipes: PVC; Expanding water stops: HE/EPDM; Screws: stainless steel V2A (AISI 304L)

Load case: Waterproof concrete stress class 2

Tightness: gastight and watertight to 1.0 bar

Tests/Standards: DVGW VP 601

Features: Reliable installation due to front panel with integrated spirit level; Visual installation reliability due to built-in inspection opening

Article Code: MSH PolySafe MV

Article number: 1560000004

GTIN: 4052487162715

Brand: Hauff-Technik

**Hauff-Technik GmbH & Co. KG**

**Manufacturer information**

Hauff-Technik GmbH & Co. KG
Robert-Bosch-Straße 9
89568 Hermaringen, GERMANY

Telefon +49 73 22 13 33 - 0
Fax +49 73 22 13 33 - 999
office@hauff-technik.de
http://www.hauff-technik.de