**ETGAR exterior sealing element for single-line building service outlet**

for ETGAR building package for single-line building service outlet

To supplement the ETGAR BHP wall version for buildings with a basement. Can be used in core drill holes in double walls/element walls and for integration of existing building seals according to DIN 18533 W2.1-E. The sealing width of 80 mm provides a seal against both the concrete shells of the double wall/element wall and the pre-mixed concrete filling.

Dimensions: OD: 160 mm; Sealing width: 80 mm

Material: Glass fibre reinforced polyamide/EPDM/stainless steel V2A (AISI 304L)

Features: Tested according to DIN 18533; Visual installation reliability due to built-in inspection opening

Article Code: HAW-E ETGAR AD

GTIN: -

Brand: Hauff-Technik

**Hauff-Technik GmbH & Co. KG**

**Manufacturer information**

Hauff-Technik GmbH & Co. KG
Robert-Bosch-Straße 9
89568 Hermaringen, GERMANY

Telefon +49 73 22 13 33 - 0
Fax +49 73 22 13 33 - 999
office@hauff-technik.de
http://www.hauff-technik.de