**KG-FIX**

Wall collar

Water barrier flange for water pressure-tight integration of waste water pipelines in floor slabs.

Material: ABS-Regranulate/TPE; 68 % regranulate

Application range: Waterproof concrete stress class 1 and 2

Tightness: pressure-tight up to 5,0 bar - corresponds to 50 m water column; radon tight

Features: quick, tool-less assembly; contains recycled plastic

Article Code: KGF

GTIN: -

Brand: Hauff-Technik

**Hauff-Technik GmbH & Co. KG**

**Manufacturer information**

Hauff-Technik GmbH & Co. KG
Robert-Bosch-Straße 9
89568 Hermaringen, GERMANY

Telefon +49 73 22 13 33 - 0
Fax +49 73 22 13 33 - 999
office@hauff-technik.de
http://www.hauff-technik.de