**Earthing fixed point**

with cross-clamp

Article Code: HEA P

GTIN: -

Brand: Hauff-Technik

Earthing fixed point for earthing connection via cross-clamp, for installation flush with formwork.

Dimensions: Conductor core: round, Ø 25 mm; Contact washer: Ø 72 mm; Distance between contact washer and cross-clamp: 120 mm

Material: Conductor core and contact washers: stainless steel V4A (AISI 316L); Cross clamp 70 x 70 mm with threaded bolt: St37 galvanised; Protective covers: PE

Application range: Waterproof concrete stress class 1 and 2

Tests/Standards: To DIN 18014; DIN EN 62305-3; VDE 0185-305-3 (with lightning protection application)

Features: Patented anti-twist protection thanks to the special shape of the contact disc

**Hauff-Technik GmbH & Co. KG**

**Manufacturer information**

Hauff-Technik GmbH & Co. KG
Robert-Bosch-Straße 9
89568 Hermaringen, GERMANY

Telefon +49 73 22 13 33 - 0
Fax +49 73 22 13 33 - 999
office@hauff-technik.de
http://www.hauff-technik.de