**Membrane injection system**

for buildings with a basement

Article Code: MIS100ND VT63

GTIN: -

Brand: Hauff-Technik

Building entry installed from the inside of the building for trenchless building connection. Can also be used for uncontrolled drilling rockets in conjunction with driving pipes OD 63 mm.

Dimensions: For core drills: ID 99 - 103 mm; For wall thicknesses: from 240 to 600 mm

Material: Front plate: glass fibre reinforced polyamide; Sealing rubber, flange, seal insert and counter-bearing: EPDM; Pipe: PVC-U; Screws and washers: stainless steel V2A (AISI 304L)

Application range: Water exposure class DIN 18533: W1-E; Waterproof concrete stress class 1 and 2

Tightness: gastight and watertight to 1.0 bar

Features: no groundwork at the property; universal building entry with membrane injection system for core holes in the most common types of wall; Controlled resin discharge through slotted membrane hose

**Hauff-Technik GmbH & Co. KG**

**Manufacturer information**

Hauff-Technik GmbH & Co. KG
Robert-Bosch-Straße 9
89568 Hermaringen, GERMANY

Telefon +49 73 22 13 33 - 0
Fax +49 73 22 13 33 - 999
office@hauff-technik.de
http://www.hauff-technik.de